## Slide 2
Cyclotron
Resonance
Antenna
Cut-off surface
Evanescent
layer
Electron density ne
Plasma radius R
Cut-off
Density nc
Waves are evanescent
here
Core
plasma
Unconfined plasma
Waves are propagative
here

## Slide 5
Chart: RF duration [s]
| 10 | 60 | 30 | 3600 | 16 | 600 | 1200 | 600 | 600 | 300
Working Points | 4.4923 | 6.1656 | 2.8937 | 4.5473 | 7.0736 | 3.1554 | 3.2354 | 4.5473 | 5.1839 | 4.7286
ITER Targets | 3.0607 | 3.3583 | 4.2726
ITER Targets
ITER Tests
2016
JET-ILA
2003
1st CW tests
2004
Dry air
(IPP)
ITER Tests
2012
Trans.Lines
2006
RF+sliding
2009
ITER Tests
2012
ITER Tests 2012
ITER Tests 2016

## Slide 6
New CuCrZr louver
RF Tested CuCrZr louver
28 µm
11 µm

## Slide 7
RC=(ρ1 + ρ2) /4a
ρ1
ρ2
RF conductor B
RF contact louver
RF conductor A
I

## Slide 8
Parameter | value
Contact Force | 6N-30N
Sliding speed | 0-10mm/s
Stroke | ±20mm (Max)
Operating temperature | ≤250ºC (steady-state) 250 ºC -350 ºC short period
Vacuum | 1atm-10-5Pa
HV-MTEST:
  ITER RF contact relevant working conditions are mimicked.
  Normal contact force can be adjusted gradually in vacuum.
  CoF& Rc simultaneous measurement.
HV-MTEST tribometer

## Slide 9
Outer Conductor
Inner Conductor
RF Contacts

## Slide 11
Fix Part
louver
Moving Part
Creeping
RF Current
Functional coating #1
Functional coating #2
Bulk material #2
Bulk material #1

## Slide 16
15
Septum 9

## Slide 17
Stage 2
Stage 1
Bridge
Feeder 30Ohm
Capacitors
Straps+
"plasma"
Impedance Transformer
Service Stub
0
0
0
IZ=0ohm
PNUM=1
RZ=30ohm
DI=190mm
DO=214mm
P=20mm
ER=1
DI=190mm
DO=214mm
P=20mm
ER=1
DI=2*235mm
DO=2*246mm
P=L3
ER=1
DI=Stage2_Dint
DO=2*246mm
P=d1
ER=1
DI=170mm
DO=214mm
P=30mm
ER=1
DI=170mm
DO=214mm
P=30mm
ER=1
DI=Stage2_Dint
DO=Stage2_Dout
P=L2
ER=1
DI=Stage1_Dint
DO=Stage1_Dout
P=L1
ER=1
DI=140mm
DO=230mm
P=200mm
ER=1
A
Name=I2
A
Name=I3
V
Name=V2
V
Name=V3
V
Name=VT
A
Name=IT
C=69.3186156951009pF
R=0.01
R=20000000
L=2.4e-008
L=2.4e-008
R=20000000
R=0.01
C=81.9301249915538pF
R+jX
RZ=1.08meter
IZ=30ohm
R+jX
RZ=1.08meter
IZ=30ohm
DI=56mm
DO=150mm
P=1350mm
ER=1
net_T

## Slide 19
153
140
114
153
Feedthrough
Service-stub
(inner conductor
water cooling)
Toward
Generator
(30 Ω line)
Toward
Antenna
Front-face
5.3 Ω Section
17.6 Ω Section